Effect of annealing temperature on Cu2O thin films prepared by thermal oxidation method.

Tran Thi Ha1,2, Nguyen Thi Huyen Trang2, Bach Thanh Cong2,

Nguyen Thi Dieu Thu1, Nguyen Thanh Binh2, Pham Nguyen Hai2#,  NguyenViet Tuyen2,*

1Department of Physics, Faculty of Basic Science, University of Mining and Geology, Duc Thang, Tu Liem, Hanoi

2Faculty of Physics, Vietnam National University- University of Science, 334 Nguyen Trai, Thanh Xuan, Hanoi

Email: #phamnguyenhai@hus.edu.vn; *nguyenviettuyen@hus.edu.vn;

Abstract: We report a facile process to fabricate cuprous thin film by thermal oxidation of copper substrate. Structure and phase identification were studied by Xray diffraction measurement and Raman spectroscopy. Scanning electron microscopy was utilized to study surface morphology of the as-fabricated thin films and optical properties of the sample was investigated with diffused reflectance spectroscopy. The study shows that cuprous thin films could be obtained by controlling annealing temperature in region of 200-300 oC.

Keywords: copper oxide; thin films; thermal oxidation; Raman

- Introduction:

Cuprous oxide (Cu2O) is a semiconductor with bandgap of around 1-2 eV [1], which finds many applications in fields of sensor, photocatalyst and especially photovotaics [2–8] thanks to their interesting properties such as: earth abundant composition, environment friendly, high absorption coefficient in visible region, p type conduction.  Even though the efficiencies of solar cell based on copper oxide is often quite low of around 1-2%, the ratio of efficiency to cost of Cu2O is still very competitive to other materials. Hence, preparation of Cu2O thin film is an interesting topic for study from both fundament and application point of view.

Various techniques were developed to fabricate Cu2O thin films for example: electro-deposition, chemical oxidation, reactive sputtering, reactive chemical deposition [4,9–14]… However, to realize such applications, a cost effective fabrication process is very important. In this paper, we report a one-step process to fabricate high quality cuprous thin films by thermal oxidation and investigate the influence of annealing temperature on the structure and some properties of the materials.

- Experiment

Cuprous oxide thin films were prepared on high purity copper substrates. Diluted HCl acid (10%) solution was first used to remove native oxide layer on copper substrate. The substrates were then rinsed thoroughly with distilled water. Thermal oxidation of copper substrate was performed in an electrical furnace XD-1600MT. The annealing time was set at various temperatures in range of 200-300 oC. Surface morphologies of the as-produced thin films were studied by using Nova Nano SEM 450. Raman spectra of samples were acquired on Labram 800 from Horiba. The samples were excited with 632.8 nm line of He-Ne laser. All spectra were taken at room temperature with acquisition time of 30s and low power at surface sample of 0.5 mW. Structure and phase identification of the samples were investigated by Xray diffractometer Bruker D500, using monochromatic wavelength (1.54056 Å) of Cu Kα radiation. Energy dispersive Xray spectroscopy integrated on SEM system was used to verify elemental composition of the sample. Optical properties of the samples were characterized with diffuse reflectance spectroscopy.

- Results and discussion:

(a) 						(b)

(c)

Figure 1. Raman spectra of copper oxide thin films prepared at 200 oC (a); 250 oC (b) and 300 oC in different times.

Figure 1 shows Raman spectra of copper oxide thin films prepared at different temperatures and times. Several Raman features were observed in the region from 100 to 600 cm-1. Three characteristic peaks of CuO appeared at 288 cm-1, 330 and 621 cm-1, which can be assigned to the Ag, B1g  and B 2g  modes, respectively [15,16]. Other Raman peaks in region 100-300 cm-1 belong to Cu2O as reported [17–19]. It should also be noted that according to group theory, cuprous oxide has one Raman active mode at 600 cm-1. However this Raman mode was not observed in the spectra of these samples. Some other Raman features were observed at around 200 cm-1. These Raman modes are believed to related to defects in this Cu2O materials, which are reponsible for p type conduction in Cu2O [19,20].

As can be seen from Raman spectra in Figure 1,  after 30 min of annealing, both CuO and Cu2O were formed. As increasing annealing time to 60 min, the intensity of the peaks of Cu2O increased notably and became dominant in the spectra. At longer annealing time and higher temperature, the peaks of CuO became weaker and weaker. At annealing time of 150 min, the most intense peak of CuO at 290 cm-1 almost disappeared for samples annealed at 300 oC. We understand that 300 oC the crystal growth rate of Cu2O is higher than that of CuO and even though the obtained thin films are composed of both Cu2O and CuO, Cu2O becomes dominant at the latter stage of the growth and might form a layer of Cu2O on top of the films.

Figure 2. SEM image of copper oxide thin film prepared at 300 oC in 150 min

Figure 3. Energy dispersive spectrum of copper oxide thin film prepared at 300 oC in 150 min

SEM image of copper oxide thin film annealed in 150 min is shown in Figure 2. It can be seen that the obtained film contains no crack or holes. The top view image demonstrates that the film is composed of nanocrystals. The purity of the sample was verified by the fact that only oxygen and copper peaks appear in the EDS spectrum.

(a)					(b)

Figure 4. Diffuse reflectance spectra (a) and F(R) vs wavelength plot (b) of  thin films prepared at 300 oC in different times.

(a)				        (b)

Figure 5. Plot of (F(R).hv)2 vs hv (a) and bandgap values (b) of the samples annealed at 300 oC in different times.

Figure 4 shows diffuse reflectance spectra and the plot of absorption coefficient F(R) calculated from reflectance data by using Mubelka Munk function. From the absorption coefficient, the plot of (F(R)hv)2 vs. hv was built to estimate the bandgap of the as-prepared films. Band gap values are extrapolated from intersection between the linear fit of the graphs with the energy axis.

The results show that band gap gradually reduces as heating time decreases. Bandgap of the films tends to remain unchanged at heating greater than 120 min. The results can be understood that at long annealing time, Cu2O is the dominant phase in the sample as shown by Raman data. The bandgap value of the films is closed to the optimal value for solar absorber layer for solar cell.

- Conclusion:

High quality thin films of cuprous oxide were successfully fabricated on copper substrate by thermal oxidation method. The results showed that annealing temperature and annealing time are critical parameters to get thin films of pure phase. The as-prepared copper oxide thin films has band gap of around 1.4 eV, which is optimum for solar absorbing materials and hence are very promising in electronic and photovoltaics applications.

Acknowledgement:

This research is funded by Vietnam National Foundation for Science and Technology Development (NAFOSTED) under grant number 103.02-2017.351

References:

[1]	Y. Wang, S. Lany, J. Ghanbaja, Y. Fagot-Revurat, Y.P. Chen, F. Soldera, D. Horwat, F. Mücklich, J.F. Pierson, Electronic structures of Cu2O, Cu4O3, and CuO: A joint experimental and theoretical study, Phys. Rev. B. 94 (2016) 1–10. doi:10.1103/PhysRevB.94.245418.

[2]	K. Mikami, Y. Kido, Y. Akaishi, A. Quitain, T. Kida, Synthesis of Cu2O/CuO nanocrystals and their application to H2S sensing, Sensors (Switzerland). 19 (2019) 1–14. doi:10.3390/s19010211.

[3]	M. Hara, Cu2O as a photocatalyst for overall water splitting under visible light irradiation, Chem. Commun. 2 (1998) 357–358. doi:10.1039/a707440i.

[4]	N. Dasineh Khiavi, R. Katal, S. Kholghi Eshkalak, S. Masudy-Panah, S. Ramakrishna, H. Jiangyong, Visible Light Driven Heterojunction Photocatalyst of CuO–Cu2O Thin Films for Photocatalytic Degradation of Organic Pollutants, Nanomaterials. 9 (2019) 1011(1)-1011(12). doi:10.3390/nano9071011.

[5]	H.M. Wei, H.B. Gong, L. Chen, M. Zi, B.Q. Cao, Photovoltaic Efficiency Enhancement of Cu2O Solar Cells Achieved by Controlling Homojunction Orientation and Surface Microstructure, J. Phys. Chem. C. 116 (2012) 10510–10515.

[6]	Y. Ievskaya, R.L.Z. Hoye, A. Sadhanala, K.P. Musselman, J.L. MacManus-Driscoll, Improved Heterojunction Quality in Cu2O-based Solar Cells Through the Optimization of Atmospheric Pressure Spatial Atomic Layer Deposited Zn1-xMgxO, J. Vis. Exp. (2016) 1–7. doi:10.3791/53501.

[7]	N. Winkler, S. Edinger, J. Kaur, R.A. Wibowo, W. Kautek, T. Dimopoulos, Solution-processed all-oxide solar cell based on electrodeposited Cu2O and ZnMgO by spray pyrolysis, J. Mater. Sci. 53 (2018) 12231–12243. doi:10.1007/s10853-018-2482-2.

[8]	T.H. Tran, V.T. Nguyen, Copper Oxide Nanomaterials Prepared by Solution Methods, Some Properties, and Potential Applications: A Brief Review, Int. Sch. Res. Not. 2014 (2014) 1–14. doi:10.1155/2014/856592.

[9]	T.H. Tran, V.T. Nguyen, Phase transition of Cu2O to CuO nanocrystals by selective laser heating, Mater. Sci. Semicond. Process. 46 (2016) 6–9. doi:10.1016/j.mssp.2016.01.021.

[10]	T.T. Ha, N. Thi, H. Trang, N.M. Hong, N.V. Tuyen, Fabrication of thin cuprous oxide layer on copper substrate by thermal oxidation method, Proc. IWNA 2017, 08-11 Novemb. 2017, Phan Thiet, Vietnam. (2017) 391–393.

[11]	I.S. Brandt, M.A. Tumelero, S. Pelegrini, G. Zangari, A.A. Pasa, Electrodeposition of Cu2O: growth, properties, and applications, J. Solid State Electrochem. 21 (2017) 1999–2020. doi:10.1007/s10008-017-3660-x.

[12]	D.S. Zimbovskii, B.R. Churagulov, Cu2O and CuO Films Produced by Chemical and Anodic Oxidation on the Surface of Copper Foil, Inorg. Mater. 54 (2018) 660–666. doi:10.1134/S0020168518070208.

[13]	S. Dolai, S. Das, S. Hussain, R. Bhar, A.K. Pal, Cuprous oxide (Cu2O) thin films prepared by reactive d.c. sputtering technique, Vacuum. 141 (2017) 296–306. doi:10.1016/j.vacuum.2017.04.033.

[14]	M.D. Susman, Y. Feldman, A. Vaskevich, I. Rubinstein, Chemical deposition of Cu2O nanocrystals with precise morphology control, ACS Nano. 8 (2014) 162–174. doi:10.1021/nn405891g.

[15]	T.H. Tran, V.T. Nguyen, Phase transition of Cu2O to CuO nanocrystals by selective laser heating, Mater. Sci. Semicond. Process. 46 (2016) 6–9. doi:10.1016/j.mssp.2016.01.021.

[16]	T.T. Ha, B.T. Huyen, N.V. Tuyen, Preparation of Well-aligned CuO Nanorods by Thermal Oxidation Method, 32 (2016) 40–44.

[17]	D.T.M. Huong, N.H. Nam, L. Van Vu, N.N. Long, Preparation and optical characterization of Eu3+ doped CaTiO3perovskite powders, J. Alloys Compd. 537 (2012) 54–59. doi:10.1016/j.jallcom.2012.05.087.

[18]	H. Solache-Carranco, G. Juarez-Diaz, M. Galvan-Arellano, J. Martinez-Juarez, G. Romero-Paredes R., R. Pena-Sierra, Raman scattering and photoluminescence studies on Cu2O, in: 2008 5th Int. Conf. Electr. Eng. Comput. Sci. Autom. Control. CCE 2008, 2008: pp. 421–424. doi:10.1109/ICEEE.2008.4723375.

[19]	T. Sander, C.T. Reindl, P.J. Klar, Breaking of Raman selection rules in Cu2O by intrinsic point defects, Mater. Res. Soc. Symp. Proc. 1633 (2014) 81–86. doi:10.1557/opl.2014.47.

[20]	T. Sander, C.T. Reindl, M. Giar, B. Eifert, M. Heinemann, C. Heiliger, P.J. Klar, Correlation of intrinsic point defects and the Raman modes of cuprous oxide, Phys. Rev. B - Condens. Matter Mater. Phys. 90 (2014) 1–8. doi:10.1103/PhysRevB.90.045203.