Research on adsorption of Ni(II) ions from aqueous solution by halloysite clay

Le Thi Duyen1,3, Le Thi Phuong Thao1,3, Nguyen Viet Hung1,3 Cong Tien Dung1, Ha Manh Hung1, Nguyen Thi Thanh Thao2,3, Bui Hoang Bac2,3

1 Department of Chemistry, Faculty of Basic Science, Hanoi University of Mining and Geology, Vietnam

2 Faculty of Geosciences and Geology Engineering, Hanoi University of Mining and Geology, Vietnam

3 HiTech-CEAE Research Team, Hanoi University of Mining and Geology, Vietnam

*Corresponding author: lethiduyen@humg.edu.vn

ABSTRACT

Nickel is a useful metal, people's demand for nickel is increasing while nickel mines are increasingly exhausted. It is essential to recover nickel from waste sources to avoid environmental pollution and utilize it. In this work, we research on the ability adsorption of Ni(II) ions from aqueous solution using halloysite clay (abbreviation is HAL), which was took from Thach Khoan area, Phu Tho, Vietnam. The light-yellow HAL powder had a specific surface area of 20.152 m2/g with particle sizes of approximately < 32 µm. The effect of factors on the Ni(II) adsorption property was investigated in aqueous solution by varying pH, the contact time, the adsorbent dose and the initial concentration of Ni(II) ions. The adsorption efficiency and capacity under suitable adsorption conditions (0.8 g HAL mass per 50 mL solution, 40 mg/L initial concentration of Ni(II), 80 minutes of contact time, pH0 of 5.9, and a room temperature of 30 oC) obtained 85.79 % and 2.145 mg/g, respectively. The results of adsorption stoichiometry of Ni(II) ions on the HAL adsorbent was fitted to the Langmuir adsorption isotherm model (R2 = 0.9931) with the maximum monolayer adsorption capacity of 3.739 mg/g. The adsorption process obeyed a pseudo-second-order kinetic model with R2 = 0.9911.

Keywords: Adsorption, halloysite, Ni(II) ions.