## Slide 1
EXPERIMENTAL and methodology
Synthesis of HAp powder
Characteristics of materials powder by methods such as: SEM, TEM, XRD, EDX, FT-IR, BET.
Cd2+ ions concentration were quantified using the ICP-MS method.
Adsorption of Cd2+ using HAp powder
The effect impacts on adsorption process was investigated including:
- the contact time changed between 10 and 100 mins;
- the initial pH of the solution was studied between 2.7 and 7.5;
- the mass of HAL in the range of 0.01 - 0.08 g/50 mL Cd2+ solution;
- initial concentration of Cd2+ in the range of 10 - 100 mg/L.
The experiments were carried out at room temperature and kept stirring at a speed of 400 rpm.
Adsorption capacity and efficiency are calculated as follow:
Q = (Co - C) x V/m; H = ((Co - C)/Co) x 100
Removal of Cd2+ from aqueous solution using hydroxyapatite: study on adsorption-desorption and recovery of cadmium
Le Thi Duyen1,2,3*, Le Thi Phuong Thao1,2,3, Nguyen Viet Hung1,2,3, Ha Manh Hung1,2, Vo Thi Hanh1,2,3, Nguyen Thi Thu Hien1,2,3, Vu Kim Thu1,3, Nguyen Thi Kim Thoa1,2, Vu Thi Minh Hong1, Le Thi Vinh1,2, Nguyen Thu Ha1, Đinh Thi Mai Thanh4, Nguyen Thi Lan Anh5
INTRODUCTION
Growth in the economy, industry, and technology releases more toxins into the environment, which contaminates water supplies. Because of its toxicity to aquatic creatures and the environment at low concentrations, as well as its persistence and bioaccumulation, heavy metal pollution is particularly concerning. Adsorption is a practical way to eliminate heavy metals that is simple to use, affordable to operate, and offers a wide variety of adsorbents to select from based on the adsorbent's requirements and the specific needs of treated water quality.
Fig. 4. Langmuir (a) and Freundlich (b) isotherm plots for the adsorption of Cd2+ onto HAp
THE 12nd VIETNAM NATIONAL CONFERENCE ON CATALYSIS AND ADSORPTION
The 3rd Vietnam - Taiwan Joint Symposium on Catalysis
Ba Ria- Vung Tau, May 23-25, 2024
1Department of Chemistry, Faculty of Basic Science, Hanoi University of Mining and Geology, No.18 Vien Street - Duc Thang Ward - Bac Tu Liem District - Hanoi, Vietnam
2BSASD Research Group, Faculty of Basic sciences, Hanoi University of Mining and Geology, Vietnam
3HiTech-CEAE Research Team, Hanoi University of Mining and Geology, Vietnam
4University of Science and Technology of Hanoi, Vietnam Academy of Science and Technology, 18 Hoang Quoc Viet Road, Cau Giay District, Hanoi, Vietnam
5Facculty of analytical engineering, Viet Tri University of Industry, No. 9 Tien Son Road – Tien Cat Ward - Viet Tri – Phu Tho, Vietnam
Logo
CONTACT
Address: Hanoi University of Mining and Geology, Hanoi, Vietnam
Email: lethiduyen@humg.edu.vn
Mobilephone: 0978 406 866
Fig. 3. The effect of contact time (a), pH (b), mass of HAp (c) and Cd2+ initial concentration on the HAp’s adsorption of Cd2+
RESULTS AND DISCUSSION
CONCLUSIONS
Hydroxyapatite obtained from chemical synthesis method, was used to remove Cd2+ ions from aqueous solution and investigate the effects of different factors on the adsorption capacity and efficiency of HAp for Cd2+ ions. The optimal conditions were determined such as 0.05 g mass of HAp per 50 mL of solution, initial Cd2+ concentration of 50 mg/L, contact time of 60 min, pH 6.5, and room temperature (25°C). Under these conditions, the adsorption efficiency and capacity obtained 94.994% and 47.497 mg/g, respectively. The results of adsorption isotherms showed that adsorption of Cd2+ ions using HAp powder followed Langmuir isothermal model with the maximum mono layer adsorption capacity of 84.034 mg/g. The experiment data of adsorption kinetics confirmed that Cd2+ adsorption process followed the pseudo-second-order law with the correlation coefficient (R2) of 0.9998. Desorption experiments were conducted with a deep eutectic solvent based on choline chloride and urea (reline) by electrochemical method. The results showed that 96.40% of Cd metal could be recovered from 0.1 g Cd-HAp by electrodeposition after 10 h, using a cathode current density of 5 mA/cm2 at 60°C. The HAp material was successfully regenerated after the desorption process.
REFERENCES
1. Ali, H., et al., Journal of Chemistry 2019 (2019) 1. 10.1155/2019/6730305
2. Wang, Z., et al., Environ Pollut 331 (2023) 121845. 10.1016/j.envpol.2023.121845
3. Praipipat, P., et al., Arabian Journal of Chemistry 16 (2023). 10.1016/j.arabjc.2023.104640
4. Pai, S., et al., Journal of Water Process Engineering 38 (2020) 101574. 10.1016/j.jwpe.2020.101574
Sponsor
by
Organized by
Pseudo-first-order kinetic equation |  |  | Pseudo-second-order kinetic equation |  |  | Qe,exp
Qe | k1 | R2 | Qe | k2 | R2 | 
17.059 | 0.05710 | 0.9045 | 71.942 | 0.00776 | 0.9998 | 70.648
Langmuir |  |  | Freundlich |  | 
Qm | KL | R2 | n | KF | R2
84.034 | 0.8151 | 0.9957 | 3.3478 | 35.0649 | 0.9643
J, mA/cm2 | H, % |  | mCd-HAp, g | H, % | t, hour | H, % | t, oC | H, %
t = 5 h; mCd-HAp = 0.3 g; T = 60oC |  |  | J = 5 mA/cm2; t = 5 h; T = 60oC |  | J = 5 mA/cm2; mCd-HAp = 0.1 g; T = 60oC |  | J = 5 mA/cm2; mCd-HAp = 0.1 g; t = 8 h | 
1 |  | 49.83 | 0.1 | 86.67 | 2 | 75.36 | 50 | 86.35
2 |  | 58.79 | 0.2 | 78.62 | 3 | 78.62 | 60 | 94.12
3 |  | 65.82 | 0.3 | 72.69 | 4 | 83.07 | 70 | 94.79
5 |  | 72.69 |  |  | 5 | 86.67 |  | 
7.5 |  | 73.32 |  |  | 6 | 89.98 |  | 
 |  |  |  |  | 8 | 94.12 |  | 
 |  |  |  |  | 10 | 96.40 |  | 
Desorption of Cd2+ ions and recovery of metallic Cd by electrochemical precipitation
Deep eutectic solvent (DES) of reline was made from choline chloride (ChCl) and urea (U). The two solid chemicals were mixed with a molar ratio of 1:2 and stirred at 60oC for 3 h until a colorless and homogeneous liquid was obtained.
Ca/P = 1,629;
Ca/P/O = 10/6,139/25,426
Fig. 1. The SEM image, EDX, XRD, FT-IR and pHPZC results of fabricated HAp powder
pHpzc = 7,49
Fig. 5. The description of the experimental data according to pseudo-first-order kinetic equantion (a) and pseudo-second-order kinetic equantion (b) for adsorption of Cd2+ onto HAp
Table 2. Adsorption isotherm parameters
Table 3. Adsorption kinetic parameters
The appropriate adsorption conditions: 0.05 g HAp/50 mL Cd2+ solution of 50 mg/L, contact time of 60 minutes at natural pH 6.5, room temperature (25oC).
Synthetic HAp material is powdery, white, rod-shaped, and very homogeneous, with particle sizes of roughly 20 x 50 nm. The chemical composition is compatible with the molecular formula Ca10(PO4)6(OH)2, pHpzc = 7.49, and surface area calculated by BET of 91.42 m2/g.
The HAp material retains its rod-like structure during adsorption, although the composition contains Cd.
Fig. 2. The SEM image and EDX results of Cd2+ absorbed-HAp
The adsorption of Cd2+ ions by HAp powder
The desorption process of Cd2+ from Cd2+ adsorbed-HAp and recovery of Cd by electrocdeposition method in reline electrolyte
WE | Au (S = 0.0201 cm2)
RE | Ag,AgCl¦Cl-
CE | Pt
Potential step | 0,005 V
Scanning rate | 0,02 V/s
 | Cd2+/reline | Cd-HAp/reline
Potential range | 0.1 ÷ -0.9 (V) | -0.2 ÷ -1.2 (V)
Vreline | 10 mL | 10 mL
Cd2+ concentration | 0.005 M | -
mCd-HAp | - | 1.0 g
Table 4. CV scanning parameters
Fig. 6. CV curves of Cd2+ and Cd-HAp in reline
Table 5. . The effect of factors on desorption Cd2+ and recovery Cd from Cd-HAp in reline
Fig. 7. Cathode polarization curve of Au electrode in Cd-HAp/reline at 5 mA/cm2 for two hours at 60oC
Fig. 8. The SEM image and EDX result of the surface of Au electrode after Cd-HAp electrolysis
WE | Au (S = 1 cm2)
RE | Ag,AgCl¦Cl-
CE | Pt grid
Vreline | 5 mL
Table 1. Electrolysis parameters
Calcium hydroxyapatite or hydroxyapatite (HAp), which has the formula of Ca10(PO4)6(OH)2 (HAp), is a material widely used in life. Because of having high activity and biocompatibility, synthetic HAp is widely used as a biomedical material in surgery of bone grafting, orthopedic, and tooth repair, as well as in the field of environmental treatment with high efficiency.
Along with adsorption, desorption and recovery of heavy metals are also extremely important to avoid secondary pollution, to reuse useful metals from waste sources and regenerate adsorbent materials, improving economic efficiency. This report presents the results of an investigation into the feasibility of using synthetic hydroxyapatite material to adsorb Cd2+ ions in water. The desorption and recovery of metallic Cd were next studied with electrochemical precipitation in a reline electrolyte.