## Slide 1
Toi Trung Tran, Thanh-Hai Pham*, Thuat Tien Phung
Department of Mineral processing, Faculty of Mining, Hanoi University of Mining and Geology
Research on hydrometallurgy technology to recover copper in fine solid waste slurry from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 2
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Diagram for printed circuit board manufacturing process

## Slide 3
Diagram of industrial wastewater treatment by precipitation method
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 4
High temperature treatment
Thermal treatment by plasma
Pyrometallurgy
Hydro metallurgy
Waste sludge treatment methods
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Waste sludge treatment in order to recover the valuable elements

## Slide 5
No. | Analytical criteria | Unit | Grade content | No. | Analytical criteria | Unit | Grade content
1 | Al2O3 | % | 0.35 | 19 | Cu | ppm | 240,576.8
2 | CaO |  | 14.35 | 20 | Ga |  | < 10
3 | Fe2O3 |  | 21.28 | 21 | Ge |  | < 20
4 | K2O |  | 0.01 | 22 | La |  | < 5
5 | MgO |  | 1.91 | 23 | Li |  | < 5
6 | MnO |  | 0.25 | 24 | Mo |  | < 5
7 | P2O5 |  | 0.04 | 25 | Nb |  | < 5
8 | TiO2 |  | 0.31 | 26 | Ni |  | 3,916.6
9 | Ag | ppm | < 2 | 27 | Pb |  | 139.6
10 | As |  | < 20 | 28 | Sb |  | < 10
11 | B |  | < 10 | 29 | Sc |  | < 5
12 | Ba |  | 489.1 | 30 | Sn |  | < 10
13 | Be |  | < 5 | 31 | Sr |  | 226.1
14 | Bi |  | < 10 | 32 | Ta |  | 32.7
15 | Cd |  | < 2 | 33 | V |  | 5.1
16 | Ce |  | < 5 | 34 | W |  | < 20
17 | Co |  | 121.9 | 35 | Y |  | 11.0
18 | Cr |  | 39.2 | 36 | Zn |  | 1,495.3
Chemical composition of waste sludge sample
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 6: Stage 1. Leaching process
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Flowchart of copper leaching experiment from sample

## Slide 7
Chart: The acid concentration in mol/l
| 0.5 | 1 | 1.5 | 2
Cu leaching efficiency | 72.68 | 87.44 | 94.73
Cu grade content in residue | 7.94 | 4.93 | 2.59
The effect of the acid concentration on the Cu leaching efficiency and Cu grade in residue
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Chart: The solid/liquid ratio
| 1/4 | 1/6 | 1/8 | 1/10
Cu leaching efficiency | 87.44 | 92.28 | 98.91 | 99.24
Cu grade content in residue | 4.93 | 4.14 | 0.74 | 0.52
The effect of the solid/liquid ratio on the Cu leaching efficiency and Cu grade in residue

## Slide 8
The effect of the leaching time on the Cu leaching efficiency and Cu grade in residue
Chart: The leaching time in minutes
| 30 | 60 | 90 | 120
Cu leaching efficiency | 95.65 | 98.91 | 99 | 99.09
Cu grade content in residue | 2.21 | 0.74 | 0.7 | 0.65
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Chart: The leaching temperature in OC
| 30 | 40 | 50 | 60
Cu leaching efficiency | 98.91 | 98.93 | 99.05 | 99.07
Cu grade content in residue | 0.74 | 0.72 | 0.7 | 0.71
The effect of the leaching temperature on the Cu leaching efficiency and Cu grade in residue

## Slide 9
Chemical composition of pregnant solution after leaching in the optimal conditions
No. | Analytical criteria | Unit | Grade content | No. | Analytical criteria | Unit | Grade content
1 | Al | mg/l | 70.83 | 19 | Cu | mg/l | 29,723.6
2 | Ca |  | 586.49 | 20 | Ga |  | < 0.01
3 | Fe |  | 4,284.84 | 21 | Ge |  | < 0.01
4 | K |  | 19.39 | 22 | La |  | < 0.01
5 | Mg |  | 1,247.98 | 23 | Li |  | 0.1
6 | Mn |  | 215.36 | 24 | Mo |  | 0.4
7 | P |  | 10.92 | 25 | Nb |  | < 0.01
8 | Ti |  | 34.44 | 26 | Ni |  | 251.3
9 | Ag |  | 1.9 | 27 | Pb |  | < 0.01
10 | As |  | 2.2 | 28 | Sb |  | < 0.01
11 | B |  | < 0.01 | 29 | Sc |  | 0.2
12 | Ba |  | 3 | 30 | Sn |  | < 0.01
13 | Be |  | < 0.01 | 31 | Sr |  | 4.8
14 | Bi |  | < 0.01 | 32 | Ta |  | < 0.01
15 | Cd |  | < 0.01 | 33 | V |  | 0.5
16 | Ce |  | < 0.01 | 34 | W |  | < 0.01
17 | Co |  | 5.8 | 35 | Y |  | 0.2
18 | Cr |  | 1.6 | 36 | Zn |  | 35.1
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 10: Stage 2. Copper cementation
Flowchart for copper cementation by iron shavings
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 11
The effect of the amount iron shavings to the copper cementation efficiency and the amount Cu2+ in barren solution
Chart: The ratio of amount Fe/ Cu2+
| 1 | 1.2 | 1.5 | 2 | 4
Cu recovery efficiency | 97.22 | 99.2 | 99.91 | 99.91 | 99.92
the amount Cu in barren solution | 827.6 | 238.8 | 27.5 | 25.5 | 24.2
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Chart: Cementation time in minutes
| 30 | 45 | 60 | 75 | 90
Cu recovery efficiency | 99.75 | 99.86 | 99.91 | 99.91 | 99.91
the amount Cu in barren solution | 75.3 | 40.7 | 27.5 | 27.8 | 28.01
The effect of the cementation time to the copper cementation efficiency and the amount Cu2+ in barren solution

## Slide 12
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen
Chart: Cementation temperature
| 30 | 50 | 70
Cu recovery efficiency | 99.91 | 99.91 | 99.9
the amount Cu in barren solution | 27.5 | 26.3 | 28.5
The effect of cementation temperature to the copper cementation efficiency and the amount Cu2+ in barren solution

## Slide 13
No. | Analytical criteria | Unit | Grade content | No. | Analytical criteria | Unit | Grade content
1 | Al | mg/l | 57.47 | 19 | Cu | mg/l | 27.5
2 | Ca |  | 640.4 | 20 | Ga |  | < 0.01
3 | Fe |  | 21,389.87 | 21 | Ge |  | < 0.01
4 | K |  | 3.05 | 22 | La |  | < 0.01
5 | Mg |  | 1,130.36 | 23 | Li |  | 0.1
6 | Mn |  | 343.82 | 24 | Mo |  | 0.7
7 | P |  | 74.3 | 25 | Nb |  | < 0.01
8 | Ti |  | 6.07 | 26 | Ni |  | 287.7
9 | Ag |  | < 0.01 | 27 | Pb |  | 23.8
10 | As |  | 1.9 | 28 | Sb |  | < 0.01
11 | B |  | < 0.01 | 29 | Sc |  | < 0.01
12 | Ba |  | 1.4 | 30 | Sn |  | < 0.01
13 | Be |  | < 0.01 | 31 | Sr |  | 5.3
14 | Bi |  | < 0.01 | 32 | Ta |  | < 0.01
15 | Cd |  | 0.6 | 33 | V |  | 1.9
16 | Ce |  | 0.2 | 34 | W |  | 1.7
17 | Co |  | 13.4 | 35 | Y |  | 0.3
18 | Cr |  | 12.6 | 36 | Zn |  | 46.5
Chemical composition of solution after cementation in optimal condition
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 14
Samples
Waste sludge from Samsung PCBs production factory, Thai Nguyen;
For the leaching process
The H2SO4 concentration: 1.0 mol/l; leaching time: 60 minutes, the S/L ratio:1/8; continuous stirring: ~180 rpm at room temperature;
The result: leaching efficiency:98%, the copper grade content in pregnant solution: 29.723 g/l.
Has fine particle size (100% particles passing 0.074 mm) and a copper grade content of 24.05 %.
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 15
Further works
Necessary to research iron reduction methods to obtain copper powder products with high purity;
Precipitation of over 99% copper metal from the pregnant solution.
For the successive cementation process
The amount of iron shavings/copper: 1.5; stirring continuously: 60 minutes;
The barren solution after cementation contains a high amount of iron ions (21.39%), so it needs to be reduced before being recirculated for the leaching process.
Thanh-Hai Pham| Research on hydrometallurgy technology to recover copper in fine solid waste slurry
from the electronic board manufacturing stage of Samsung factory, Thainguyen

## Slide 16
Thank you for your attention!
Contact:
Dr. Thanh-Hai Pham (Mr.)
Department of Mineral processing, Hanoi University of Mining and Geology
Address: No.18, Vien Str., Ducthang ward, Bactuliem dist., Hanoi, Vietnam
Email: phamthanhhai@humg.edu.vn
Tel: (+84) 788 268 258